Types of polymers

  - Polyvinyl acetate (PVA)

Produced from (CH3COOH) and acetylene

Properties

- linear  polymer

- amorphous structure

- Supplied as an emulsion with water

- Effectively to almost any surface

- Elastic and succulent

- Easily molded

- Tg (28 oC)

- High absorption of water

Using

- Glues and chewing

- Water dries off

- Strong adhesives

- Vinyl emulsion paints (latex)

  - Polyimide (PI) (high temp. polymer)

Properties

- ladder  polymer

- Semi crystalline  structure

- have complex ring structure units along the polymer chain these give rise to increased Vander Waals forces between the long chain molecules so that a higher temperature is necessary to cause their separation – greater heat input causes the molecules to vibrate more vigorously until they separate .

- very high heat resistance

- used in high temp

- Max temp. in use for long time  (260  oC)

- Max temp. in use for short time (10 min) (380  oC)

- Max temp. in use for short time (200 hr) (355  oC)

- Max temp. in use for short time (1000 hr) (300  oC) about (90 %) of the original tensile strength is retained

Using

- Pressure sensors

- Aerospace and electronic industries

- tapes about  wires in aeroplanes  and rockets

- rods and sheets

  - Polytetrafluoroethylene (Teflon) (PTFE)

Produced from tetrafluoroethylene gas and this gas is boredom

Properties

- linear polymer and (90 %) crystalline

- fluorine formed compounds is difficult to decompose

- high costing

- excellent electric insulator

- Sticky materials cannot adhere to it easily

- Low coefficient of friction

- Low strength

- Tough and flexible

- (2.0-2.3 g/cm3) density

- chemical inert

- good corrosion and solvent resistance

- Max temperature in use ((-260 )– (+260)  oC)

- Forming by powder metallurgy

- Don’t effect with water and vapor  until  (250 oC)

Using

- Cooking utensils , filters , piston rings and gaskets

- Bearings conduits and sealings

- Coating and coating of wires

- dry film lubricant

- tanks and pipes for acids transport

  - Polymethyl methacrylate (PMMA) (acrylics)

Produced by polymerization of methyl methacrylate .it  name (plexiglass)

Properties

- linear polymer with bulky side groups

- amorphous structure

- stiff and strong

- high Transparence polymer

- (1.18 g/cm3) density

- Max temp. in use (95 oC)

- Like glass but tougher and lighter than glass

- easily for moulded

- weather resistance

Using

- light fitting

- lenses for car lights

- sheets for baths

- lamps , dishes , sinks

- windows and replace glass in windows

- roof lighting

  - Polyacetals(polyoxymethylene) (POM)

Properties

- linear polymer with a backbone which consist of alternate carbon and oxygen atoms

- high crystalline

- two types (Homopolymer and Copolymer)

- backbone of copolymer consist ethylene units

- homopolymer stronger and stiffer than copolymer

- copolymer strength at high temp. than homopolymer

- high fixity to distances

- Low coefficient of friction

- Good wear strength

- Good resistance to moisture absorption

- (1.4 g/cm3) density

- Melting point (165 oC)

- High chemical resistance and  electric insulator

- High Impact strength  at (- 40 oC)

- High creep strength polymer

- Stiff and strong and high yield strength

- High notch sensitive

- High cost

Using

- Springs , sliding parts ,flexible shifts and pipe fittings

- Washing machines

- Bearing , gears handles and good quality toys

  - Linear Polyurethanes (PUR)

Products from chemical reaction of isocyanate and alcohol

Properties

- linear polymer

- semi crystalline structure

- melting point (160 - 190 oC)

- density (1.21 g/cm3)

Using

- small technical parts

- gear teeth

- Washing machines parts

- Artificial organs and veins