Extraction of Copper (II) from aqueous solutions by using of

2-[ (4-Bromo phenyl) azo]-4,5-diphenyl imidazole

Ahmed W.R., Nahla F. M.  and Mohamed . Kh.K.

Department of Chemistry, College of Science  , University of Kufa

(NJC)

(Recevied on 19/4 /2010) 		  (Accepted for publication   2/ 5 /2011)

Abstract

The extraction of Copper has been studied as a complex by means of 2-[ (4-Bromo phenyl) azo]-4,5-diphenyl imidazole dissolved in chloroform .The study revealed that the optimum pH value was (pHext. = 9 ), concentrations of Cu(II) ion   in   aqueous solution giving highest distribution ratio (D) were (40μg) and the ligand              [1x10-4M] respectively and the optimum shaking time to reach the equilibria was ten minutes . Studies organic solvent showed there is not any linear relation between dielectric constant of organic solvents and distribution ratio (D)  of extraction ,but there is an effect for the structure of organic solvent . The thermodynamic study demonstrates the complexation reaction is  an exothermic at temperature degrees ( 20 C 0 - 70 C0 ).

Key words: extraction , P-BrPAI ,copper, azo, imidazole.

الخلاصة

تمت دراسة عملية استخلاص ايونات النحاس (II) من المحاليل المائية بواسطة الكاشف 2- )]4- برومو فنيل ) ازو –[ 45,  ثنائي فنيل أميدازول (P-BrPAI) المذاب في الكلوروفورم فقد كان  هذا الكاشف جيد للاستخلاص  هذه  الايونات  وتضمن الدراسة النواحي الاتية :

تاثير الدالة  الحامضية  pH  حيث  كانت  القيمة المثلى  لاستخلاص ايونات النحاس الثنائية  عند pH = 9 , اما افضل تركيز للنحاس الثنائي  الذي يعطي اعلى قيمة لنسبة التوزيع ويحقق لنا حالة الاستخلاص الافضل حيث كان التركيز (40 μg)   (1.2×10-4  M ) هو افضل تركيز , اما من الجانب الحركي لتفاعل التعقيد بين ايونات النحاس  (II)والكاشف (P-BrPAI)  فقد بينت الدراسة ان زمن الرج ( 10 دقائق ) هو الافضل لوصول المعقد الى حالة الاتزان , كذلك تم دراسة تاثير تركيز الكاشف العضوي  و وجد ان افضل  قيمة لنسبة التوزيع عندما يكون التركيز1x10-4M  .كذلك تم  دراسة تاثير المذيب العضوي وظهرعموما انه لاتوجد علاقة خطية بين نسبة التوزيع للاستخلاص  و ثابت العزل الكهربائي للمذيبات العضوية المستخدمة ، كما اوضحت الدراسة الثرموديناميكية لتفاعل التعقيد  ان التفاعل باعث للحرارة من ( 70 C 0 - 20 C0 ) .

156

156

Introduction

157

157

Sensitivity and selectivity behavior of azo compounds and imidazoles as well as their derivatives for complex formation with metals as well as their extraction have been giving growing concern. Several studies were carried out on the extraction and determination of Cu (II) and complex formation by imidazoles compounds. Preparation  and  Identification  of  Some   Transition Metal Complexes with  the New  Ligand 2- [ p- (2′- Pyrimidyl  sulphamyl)  phenyl azo] - 4,5- diphenyl imidazole studied by A. J . Khadim and A.K.Hassan , using 2-[(α-naphthyl) azo]-4,5-diphenyl imidazole  to  extraction  of  copper and silver [1,2] Carolina et al., Studied the extraction of imidazole chelate complex with copper [3].  Synthesis of tri- and tetra substituted imidazoles carried by Daniel V. Paone and Anthony W. Shaw [4]. Ibolya Apro studied the complexation of Cu (II) ,Zn(II) and Ni(II) with imidazole as ligands and inositol derivatives [5]. Synthesis a new imidazole ligand  and stadied it complexes with Co(II), Cu (II) , and Ni(II)  was carried out by Ibramim and Nebahat.  [6]. The extraction of Cu(II) and Ag (I)  using 2-[(4-carboxy methyl phenyl )azo]-4,5-diphenyl imidazole and 2-[(3-methyl benzene) azo]-4,5diphenyl imidazole as well as Synthesis and Spectrophotometric    determination of  Cu  (II) ,Ni   (II) using the organic reagent 2-[ (4-Bromo phenyl) azo]-4,5-diphenyl imidazole Fig(1) was studies by I. R. Ali [7,8]. Jose´ J. Campos et al., have Studied Coordination geometry isomerism induced by N–H -Cl, C–H-Cl, C–H-N, C–H-p and p-p supra molecular interactions in mercury(II) complexes with tri pyridyl imidazole chelating ligands [9] . N. Dallali et al., have studied cloud point extraction and determination of Zn, Co, Ni and Pb by flame atomic absorption spectrometry  using 2-Guanidinobenzimidazole as the complexing agent [10]. In other study used 2-[p-(2′-Pyrimidyl sulphamyl) phenyl azo]-4,5-diphenyl imidazole to extraction of Cu(II) from aqueous solutions [11].P.Giridhar et al., have  studied  the extraction of uranium and the effect of alkyl group on the extraction [12].   As well as T.K. Mondal et al., have studied Synthesis , structure spectra and redox properties of Ruthenium–carbonyl complexes of 1-alkyl-2-(arylazo) imidazoles [13]. studies in solvent extraction of group (IIb) metal ion by new organic reagent ",2-[(4-Chloro-2- methoxy phenyl)azo]-4,5-diphenyl imidazole.were carried out by Abdul Muttalib [14].

Apparatus

TRUV754(UV – Visible Spectrophotometer) was used for absorption measurements , 3320 Jenway pH Meter was used  for pH measurements.

Materials

CuSO4.5H2O ,  Dithizone (D2HZ),   H2SO4,  NH4OH , Chloroform  , Dichloromethane, 1,2-Dichloroethane, Carbon tetra chloride , Benzene ,  and Toluene  from  B. D. H. and Merck ,The  ligand  2-[ (4-Bromo phenyl) azo]-4,5-diphenyl imidazole synthesized  .

Procedure

i-prepration of standard stock solutions

(a) A solution of Copper (II) (1 mg\ml ) was prepared by dissolving 3.928 gm CuSO4.5H2O (0.015 mol) in 1 liter of distillated water containing 1 ml of conc. H2SO4

(b) A standard solution of 1x10-4 M  of (P-BrPAI) was prepared by dissolve 0.004 gm  in 100 ml of CHCl3.

(c) A solution of 1x 10-2M of  Dithizone (D2HZ)  was prepared by dissolve 0.0256 gm  in 10 ml of CCl4.

(d) A dilute solution of  ammonia was prepared by addition 1drop of conc. ammonia in 25 ml of D. W .

ii-Calibration curve :

different concentrations  of (1– 40 ) μg of Cu(II)   were prepared using  D.W. after the solutions had been adjusted to pH ≤ 1, they were transfered to a separate funnel and were extracted with portion of H2DZ  in CCl4 with shaking it about 3 min. continuous the addition until the last portion does not  change its green colour . the removing free reagent by shaking the combined extracts with the dilute ammonia sol.after that the complex solution of Cu(HDZ)2 was diluted with CCl4 in 10ml  volumetric flask then  absorbance was measured the at 550 nm , the solvent was used as reference (Dithizone method)[15],the calibration curve was illustrated in Fig(2).

iii- Extraction of Copper (II)

A 5ml   of  aq.  solution  of  Cu(II)  has  a specific   concentration was  placed    in (25 ml) separating funnel with equivalent volume of ligand solution . after the separation funnel had been shaked  within 10 sec . the  two layer was separated  .

iv-Determination of distribution ratio

A residue of Cu(II) was  determinated using spectrophotometric method  ,then a value of  D  was calculated using the relation  ship below :

Conc. Of Cu(II) in organic phase

Distribution ratio (D) =             [16].

Conc. Of  Cu(II) in  aqua.  phase

N = N

N

N

ph

ph

H

Br

N = N

N

N

ph

ph

H

Br

2-[ (4-Bromo phenyl) azo]-4,5-diphenyl imidazole[ 8 ]

2-[ (4-Bromo phenyl) azo]-4,5-diphenyl imidazole[ 8 ]

Fig (1) : structure of ligand used in extraction method

Results and Discussion

Table (1) and Fig (3)  was shown  that, (pHex=9) was the optimum value of pH extraction. At pH less than optimum value the imidazole  molecule ligand had  been protonated to occupy the pair of electron and then can not coordinated strongly with Cu(II) ions and ion pair complex less stable and was minimized the distribution ratio (D) [3],also at pH more than optimum value distribution ratio (D) will be decreased by reason concentration of [Cu(PSPAI)]+2(HO-)2 complex was increased this complex more soluble in aqueous phase and less extracting to organic phase and it was suffered the dissociation equilibria [7] .

The optimum  Conc. Of  Cu(II)  ions  in  aqueous   phase  ,  which   is  (40μg) (1.2×10-4  M ) was illustrated by Table (2) and Fig(4).  Due to that  conc. which was giving highest distribution ratio .The conc. Of  Cu(II)  ions less than optimum Conc. was not allowed to reach the equilibria therefore, the value of D was minimized,  according to Lechatlier principle [17].

These results were demonstrated the effect of metal ion conc. on the equilibria of complexation reaction

Cu+2   +  (P-BrPAI ) + SO4-2                                          [Cu (P-BrPAI )]+2 SO4-2

158

158

Table (3) and Fig(5)  was shown that 10 minutes was the best time for shaking, this time was required to reaching the complex to equilibrium state .

The study also was illustrated of effect of P-BrPAI  concentration on the extraction process in Table (4) and Fig(6) that probability forming two species enable for extraction [Cu(P-BrPAI)]+2SO4-2) [Cu(P-BrPAI )]+2 (HO-1)2, from the  straight line slop of these species was   ( 1 : 1 ) (metal : ligand), that  the  more  probable  structure  of  ion pair  complex  was extracted  ,in Table (5) was shown the relation between dielectric constant of organic solvents and distribution ratio (D) wasn’t linear  due to extracted complex charge less and  it was affected by stereo structure of organic solvent and nature of complex soluble[18]. The  Table (6) ,(7) and Fig. (7) were demonstrated values of free energy of transition of ions from aqua. phase to organic phase and the ∆Hex. values were shown that   the  extraction   of  Cu(II)  decrease  with  increasing  temperature (i.e process is exothermic) from study different heat   degree  ( 20 C 0 - 70 C0 ) depending on (Vant- Hoff) relation ship [19]

The log Kex. verses (1/T k0) show the slope equal to  from this relation ship calculate the Value   ex.   =-27.397  kJ . mole-1

∆Gex. =-RT ln Kex.

and

∆Gex. =  ∆Hex. _ T∆ Sex.

we  used log D instead of log Kex. .

After  application of  these  relations ,  the   values   of   Gibbs   free   energy and  entropy  values showed by Table (7)  .

This result suggested  that the extraction of Cu(II) is easy and the negative value of   ∆Hex. and this mean decrease in value of ∆H solv. and increase of ∆H hyd.

[11].

While at low heat  degree (0 C0, 10 C0 )  decreasing the  distribution ratio

μg Cu(II)

Fig.(2): Calibration Curve of Cu (II)

Table ( 1 ) : Effect of pH on extraction of Cu(II) ions

| pH | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| D | 0.11 | 0.73 | 3.84 | 5.15 | 31 | 7.35 | 0.09 | ___ |
| Log D | -0.95 | -0.13 | 0.71 | 0. 58 | 1.49 | 0.86 | -1.04 | ___ |

159

159

Fig.(3): pH effect on the extraction  of  Cu(II) ions

Table(2) : Effect of Cu(II) ions concentration on the extraction method

| μg Cu(II) | 10 | 20 | 30 | 40 | 60 | 80 | 120 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ppm | 2 | 4 | 6 | 8 | 12 | 16 | 24 |
| D | 0.1 | 1.42 | 9 | 19 | 22 | 79 | 13.7 |
| Log D | -0.95 | 0.153 | 0.95 | 1.27 | 1.34 | 1.89 | 1.136 |

μg Cu(II)

Fig.(4):The effect of  Cu(II) ions concentration on the extraction method

Table ( 3 ) : Effect of shaking time on extraction of Cu(II) ions

| Time(min.) | 5 | 10 | 15 | 20 | 25 | 30 |
| --- | --- | --- | --- | --- | --- | --- |
| D | 12.33 | 31 | 25.6 | 19 | 12.3 | 12.3 |
| Log D | 1.09 | 1.49 | 1.4 | 1.27 | 1.09 | 1.09 |

160

160

Fig.(5):The effect of  shaking time on the extraction method

Table(4) : Effect of ligand concentration on the extraction method

| [ligand] x 10-5 M | 1 | 2 | 3 | 6 | 8 | 10 |
| --- | --- | --- | --- | --- | --- | --- |
| D | 3.98 | 7.16 | 25.66 | 9.66 | 9.38 | 31 |
| Log D | 0.6 | 1.1 | 1.409 | 0.97 | 1.2 | 1.49 |

Fig.(6):The effect of  ligand concentration on the extraction method

161

161

Table(5) : Effect of  organic solvent on the extraction  of  Cu(II) ions

| Organic solvent | ε | D |
| --- | --- | --- |
| 1,2-Dichloro ethane | 10.65 | 7.69 |
| Chloroform | 5.708 | 31 |
| Toluene | 2.438 | 12.33 |
| Carbon tetra chloride | 2.38 | 25.6 |
| Benzene | 2.804 | 9.66 |
| DCM | 9.08 | 16.2 |

Table(6) : Effect of  temperature on the  extraction  of  Cu(II) ions

| T οC | T οK | 1/T οK x10-3 | D |
| --- | --- | --- | --- |
| 0 | 273 | 3.6 | 25.8 |
| 10 | 283 | 3.5 | 27.4 |
| 20 | 293 | 3.4 | 31.0 |
| 30 | 303 | 3.3 | 27.5 |
| 40 | 313 | 3.2 | 20.0 |
| 50 | 323 | 3.1 | 12.5 |
| 60 | 333 | 3 | 10.0 |
| 70 | 343 | 2.9 | 7.0 |

Fig (7) : Effect of  temperature on the  extraction  of  Cu(II) ions

162

162

Table (7) :  values   of   Gibbs   free   energy  and  entropy  values of  extraction For each temperature degrees

| T k0 | ∆Hex. KJ mole-1 | ∆Gex. KJ mole-1 | ∆Sex. J mole-1 |
| --- | --- | --- | --- |
| 293 | -27.397 | - 8.344 | -65 |
| 303 |  | -8.282 | -63 |
| 313 |  | -7.777 | -62 |
| 323 |  | -6.791 | -63.7 |
| 333 |  | -6.365 | -63.1 |
| 343 |  | -5.507 | -63.8 |

References

1- A .J. Khadim ,(2006)" Preparation  and  Identification of  Some Transition   Metal    Complexes with  the new  Ligand 2- [ p- (2′- Pyrimidyl sulphamyl)  phenyl azo] - 4,5- diphenyl imidazole" M.Sc.Thesis , college  of education for girls , Kufa University.

2-A.K.Hassan,(2006)"solvent extraction of Cu and Ag asCation by use2-[(α-naphthyl) azo]- 4,5- diphenyl imidazole"M.Sc.Thesis,education forgirls college,Kufa university.

3- C. A.payer ,3E.B.Ahamirano , Inorganic chemistry  communication ,2006, 9, 901-906  .

4- D. V. Paone a , Anthony  W.  Shaw a ,  Tetrahedron Letters, 2008, 49, 6155–6159.

5-Ibolya Apro-Torok, (2002) "Copper  (II) , Zinc (II)  and Nickle(II)   complexes of    imidazole  containing   ligand and   inositol derivatives  ,  equilibrium   , structure , hydrolytic activity " Ph.D.Thesis ,university  of   Szeged .

6-Ibramim Erden and  Nebahat   Demirhan  , Uni  Avecata   separation      science   and technology, 2006, 36, 559-562.

163

163

7-I. R. Ali , (2005)"studies in  solvent  extraction  of Cu and Ag by use of ligands 2-[(4-carboxy  methyl  phenyl) azo]-4,5-diphenyl  imidazole  and 2-[(3-methyl benzene) azo]-4,5 diphenyl imidazole"M.Sc.Thesis,education for girls collage ,Kufa  university

8- I.  R.  Ali  , J. of Kufa , 2010, 1(1).

9- J. ´J .  Campos   -  Gaxiola ,  Herbert   Hopfl  , Miguel  parra - Hake ,   Inorganic chimica Acta , 2008, 361,.248-254 .

10-N. Dallali ,   M.M. Zahedi1 and    Y. Yamini  , Scientia  Iranica, 2007, 14(4),  291-296 .

11- N.F.Al-Mutawali, (2000 )"Extraction of Mo (VI) ,W (VI) by use crown ether DB18C6 ,M.Sc.Thesis, college of science, Babylon University.

12-P.Giridhar , K.A.Venkatesan, T.G. Srinivasan     and  P.R. Vasa dera Rae, J .  of Nuclear and  Radichemical sciences, 2004, 5(2), 21-26.

13-T.K.Mondal , S.K.  Sarker  , P.  Raghavaiah  , C. Sinha, Polyhedron, 2008, 27, 3020 – 3028.

14- Z.   Abdul   Muttalib , (2006)" studies   in   solvent extraction of group (IIb) metal ion by new  organic   reagent   " ,  2-[ ( 4 – Chloro - 2 - methoxy  phenyl ) azo ]-4,5- diphenyl imidazole ,M.Sc.Thesis, collage  of  education  for girls , Kufa  university

15-Z . Marczenko ,  (1976) " Separation  and Spectrophotometric   Determination   of Elements ", John  Wiley  and  Sons. Inc..

16-Marcus  and  Kerters , (1969) " Ion Exchange  and  Solvent  Extraction  of   Metal Complexs".

17- N.F.Al-Mutawali, Hurra,a. M. Al.Abidi, Abdulla  M. A., Qadisia J of  Chemistry, 2010, 24, 459-468.

18- A.Th.Salim,(2002),"Astudy on Solvent Extraction of Gadolinium (III) with Sudan Black B" M.Sc. Thesis, college of education  Ibn Al-Haitham ,Baghdad University.    19- P.W. Atkine ,  (1994) ,physical chemistry,5th ed., Oxford University , press , Uk. ,  p.109.

164

164