EFFECT OF DIE SHAPE ON THE TEMPERATURE AND STRESSES DISTRIBUTION IN THE COMPOUND

(FORWARD-BACKWARD) EXTRUSION PROCESS

Rana Ali Hussien

Pumps Engineering Department

Technical College /Al-Musaib – Iraq.

ABSTRACT

In this research the effect of the die geometry in the compound extrusion (forward – backward) process on the distribution of temperature and effective stresses is investigated; Effect of the geometrical shape of extrusion process on the power required for the forming process was also investigated. The flat surface for the punch is chosen and two types of die shape (flat and arc) are studied. The analysis of temperature and stresses distribution in the die and billet is studied using finite element method via ANSYS software. The contact region was taken into consideration. From the results, it was noted that there a tiny  changes in the pattern of temperature distribution and also a huge changes in the equivalent stress levels due to the changing in die geometry. In the backward extrusion process, a significant effect on the stress levels was also noticed due to changing in die geometry. At last, the results show that the best results of was achieved at arc die geometry .

KEYWORDS: Extrusion , Finite Element Method, ANSYS ,Temperature distribution, Stress analysis, Forward-Backward Extrusion, Compound Extrusion.

تأثير الشكل الهندسي للقالب على توزيع درجات الحرارة والاجهادات المكافئة

في عملية البثق المركب (الخلفي – الامامي)

رنا علي حسين

الكلية التقنية / المسيب – قسم هندسة المضخات

الخلاصة

في هذا البحث تم دراسة تأثير الشكل الهندسي للقالب في عمليه البثق المركب (الخلفي -الامامي ) على توزيع درجات الحرارة والاجهادات المكافئة وللتحقيق من تأثير عوامل الشكل الهندسي لعملية البثق المركب على كل من متطلبات القدرة اللازمة للتشكيل . تم اختيار شكل هندسي مسطح لرأس المكبس (المخرم) وبنوعين للشكل الهندسي للقالب (مسطح و قوس). حيث تم تحليل توزيع درجات الحرارة على القالب والمعدن ودراسة الاجهادات المكافئة وبواسطة طريقة العناصر المحددة من خلال استعمال برنامج الـ ANSYS حيث تم أخذ منطقة التلامس بين الاسطح المتلامسة بنظر الاعتبار وقد بينت النتائج  بانه يحصل تغيير طفيف في شكل توزيع درجات الحرارة نتيجة تغيير شكل القالب (مسطح و قوس) ولكن يحدث تغيير ملحوظ في الاجهادات المكافئة وايضا هناك تغيير واضح للاجهادات في البثق الخلفي نتيجة تغيير شكل القالب وان افضل النتائج كانت عندما يكون سطح القالب على شكل قوس.