Study Of Effect Of Titanium Oxide  On Some Optical Properties Of Polystyrene

Bahaa H. Rabee, Majeed Ali  ,Ahmed Hashim

Babylon University, College of Education , Department of physics,  Iraq.

Abstract

The effect of addition titanium oxide on some optical properties of polystyrene has been studied . The samples has been prepared with different weight percentages of TiO2 are(0,40,60)wt.% and different thickness .The absorption and transmission spectra has been recorded in the wavelength range (300-1100)nm . The absorption coefficient and energy gap of the indirect allowed and forbidden transition have been determined .

الخلاصة

درس تأثير إضافة  اوكسيد التيتانيوم على بعض الخواص البصرية للبولي ستايرين. ولهذا الغرض تم تحضير نماذج  بإضافة  اوكسيد التيتانيوم  إلى البولي ستايرين وبنسب وزنية مختلفة(0,40,60)wt.% من اوكسيد التيتانيوم  مع البوليمر وبسماك مختلفة.تم تسجيل طيفي الامتصاص و النفاذية و لمدى الاطوال الموجيةnm(300-1100). وقد حسب معامل الامتصاص و فجوة الطاقة للانتقالات غير المباشرة المسموحة  و الممنوعة.

Introduction

The main two types of optical transitions are direct and indirect transitions, both involve the interaction of an electromagnetic wave with the electron in valence band which may cross the forbidden gap to the conduction band [Mott N., 1971]. Indirect transitions are possible only by phonon assisted transition. The value and shape of the mobility gap in the amorphous semiconductors depend on the preparation condition such as substrate temperature, annealing temperature, degree of impurity and  defect of the material. Any variation in such parameters leads to a shift in the absorption edge towards higher or lower energy [Tauc J. ,1974]. In general the interaction of electromagnetic radiation (light) with matter is controlled by three properties, the specific conductivity, the electric conductive capacity and the magnetic inductive capacity. These properties are related to the refractive index and the absorption index of the medium. All material bodies possess a number of critical frequencies at which radiation is in resonance with some internal variation of the body. At these critical frequencies such bodies are strong absorbs of radiation, even if they are transparent to radiation on either side of the critical frequency. Among the optical properties reaction, reflection and scattering of light are the most important [ Majdi K. et.al.,1997]. Polymeric substances make up the most important class of organic materials, technically and economically. The familiar plastics, fibers, clastomers and biological materials that surround us attest to this importance. Such substances, which are composed of great many identical groups or repeating units, are known as (high polymers). Polymers composed of more than one kind of repeating units are termed copolymers [A.H.Ahmed ,2007].  In order to fulfill the requirements of polymer industry many developers usually blend polymers together in order to reach anoptimun balance of properties. this approach allows high flexibility in proerty adjustment and avoids development of new macromolecules which is generally long and expensive compared to polymer alloying [A. Mohammed, 2007].  This paper deals with results of the effect of TiO2 on the some optical properties of Polystyrene.                                      .                                                                                                  .

Experiment

The materials used in the paper is polystyrene as matrix and titanium oxide as a filler. The electronic balanced of accuracy 10-4 have been used to obtain a weight of TiO2 powder and polymer powder . These mixed by Hand Lay up and the microscopic examination used to obtain homogenized mixture . The weight percentages of  TiO2 are ( 0 , 40 and 60) wt.%. The Hot Press method is used to press the powder mixture. The mixture of  different TiO2 percentages have been compacted at temperature 185oC under a pressure 100 bar for 10 minutes . Its cooled to room temperature , the samples were disc shape of a diameter about 30mm and thickness ranged between (1.05-1.24) mm. The transmission & absorption spectra of PS- TiO2 composites have been recording in the length range (300-1100) nm using double-beam spectrophotometer (UV-210oA shimedza ).

Results and Discussion

The optical absorbance as a function of the wavelength of the incident light for PS-TiO2 composites of various filler contents is shown in figure (1) . The figure shows that the intensity of the peak increased as a result of filler addition but no shift in the peak position, i.e. adding different amounts of filler to pure polymer do not change the chemical structure of the material but new physical mixture is formed.

The absorption coefficient (α) was calculated in the fundamental absorption region from the equation[S. D. Hutagalwng and B. Y. Lee ,2007]:

Where : A  is absorbance   and d is the thickness of sample.

Figure (1) shows the relationship between the absorption coefficient and photon energy of the PS- TiO2 composites we note the change in the absorption coefficient is small at low energies this is indicates the possibility of electronic transitions is a few. At high energy , the change of absorption coefficient is large this is indicates the large Probability of electronic transitions are the absorption edge of the region                     [S. M Scholz et al,2008].

The absorption coefficient helps to conclude the nature of electronic transitions, when the high absorption coefficient values (α>104cm-1)  at high energies we expected direct electronic transitions ,and  the energy and momentum preserve of the electron and photon , when the values of absorption coefficient is low(α<104cm-1) at low energies we expected indirect electronic transitions, the momentum of the electron and photon preserves by phonon helps[B.Thangaraju and P. Kalianna,2000]. The results showed that the values of absorption coefficient of the PS- TiO2 composites less than 104cm-1  which indicates to the indirect electronic transition. The forbidden energy gap of indirect transition both allowed, forbidden calculated according to the relationship[A. Kathalingam et.al. , 2007] :

Where : hv is the energy of photon , B is proportionality constant, Eg is forbidden energy gap of the indirect transition.  If the value of (m=2)  indicates to allowed indirect transition . when the value (m=3) indicates to forbidden indirect transition. Figure (2) shows the relationship between (αhv)1/2 (cm-1.eV)1/2 and the photon energy of pure polymer (PS) , with take over part

of the straight cut oriented axis at the point (αhv)1/2 =0 will get the value of forbidden energy gap of the allowed indirect transition , which equal ( 3.1eV ). Figure (3) and    figure (4) represents the same relationship but to the polymer filled with (TiO2)   with volume  percentages of  TiO2 are (40 , 60) wt.% , the same way we can be

obtained on the value of forbidden energy gap of allowed indirect transition which equal (2.1eV) for 20 wt.% TiO2, and (1.82eV)for 50 wt.% TiO2 . we note that the

value of the forbidden energy gap decreases with increasing TiO2 concentration.. Figure(5) shows the relationship between the (αhv)1/3 (cm-1.eV)1/3 and photon energy of pure polymer (PS),the same way we obtain to the forbidden energy gap of

Indirect transition which equal (2.95eV) . Figure (6) and figure (7) represents the same relationship but to the polymer filled with (TiO2) with volume percentages of TiO2 are(40,60)wt.l%, the same way we can be obtained on the value of the forbidden

forbidden energy gap of the forbidden indirect transition which equal (1.85eV) for    40 wt.% TiO2, and (1.65eV  ) for 60 wt.% TiO2 we note that the value of the energy

gap decreases with increasing TiO2 concentration[L. I. Soliman and W. Sayed,2002].      Figure(9) shows the variations of extinction coefficient (k=λα/4π) with wave length of pure and doped PS  with TiO2 . (k) shows an increase with increasing dopant concentration. The behavior of (k) can be ascribed to high absorption coefficient. This result indicates that the dopant atoms of TiO2 will modify the structure of the host polymer. An interesting result is  TiO2 dopants increases the absorbance in the visible region[R.Ahmed,2008]

Conclusion

- The absorption coefficient of polystyrene increases with increasing of titanium oxide concentrations.

- The experimental results showed that the absorption coefficient of (PS-TiO2) composites less than 104cm-1 this is  indicates to forbidden and allowed indirect electronic transitions.

- The forbidden energy gap of polystyrene decreases with increasing of titanium oxide concentrations.

- The extinction coefficient of polystyrene increases with increasing of titanium oxide concentrations.

References

Ahmed A.H. ,2007, "Dopping effect on optical constant of polymathylmethacrlate", Eng. Technology, Vol.25 , No. 4.

Hutagalwng. S. D. and Lee. B. Y. ,2007, Proceeding of the 2nd international conference Nano/Micro Engineered and Molecular systems, January ,Bangkok,Thailand.

Heath P. and Sacher P.,1986 ,"Quality crystals and optics for laser applications", J. of Applied opt. , vol. 15 , No. 937.

Kathalingam A .et al , 2007,"Materials Chemistry and physics, vol.106,No.215.

Mohammed A.,2007, "Improvement of thermal properties for binary systems PVF-Ph, PVF-B by addition of silicon carbide", Eng. Techn., Vol. 25, No.7.

Majdi K, Zeedan K. and Attar H., 1997,"Optical properties of poly thiophene/ PVC conducting polymer alloy films", Iraqi J. of polym., Vol. 1, No. 1,155-162.

Mott N, "Electrical processes in non-crystalline materials", Clarendon Press, Oxford, 1971.

Scholz. S.M, Carrot.G and Hilborn.J ,2008, "Optical properties of Gold-Containing poly (Acrylic Acid) composites" , Lausanne, Switzerland.

Soliman . L. I and Sayed. W. M,2002,"Some physical properties of Vinylpyridine Carbon-Black composites", Cairo, Egypt.

Thangaraju B. , Kalianna P. ,2000, Cryst. Res. Techon., vol. 35, No.71.

Tauc J. ,"Amorphous and liquid semiconductors", Plenum Press, London, New York, 1974.

# Text boxes

Photon energy(eV)

λ (nm)

Figure (3) the relationship between (αhv)1/2(cm-1.eV)1/2  and photon energy of PS- TiO2 composites  for 40 wt..% TiO2

(αhv)1/3(cm-1.eV)1/3

(αhv)1/3(cm-1.eV)1/3

Photon energy(eV)

Figure (5) the relationship between (αhv)1/3(cm-1.eV)1/3  and photon energy of pure polymer (PS).

(αhv)1/2(cm-1.eV)1/2

Photon energy(eV)

Absorbance(arbitrary units)

Figure (9)  the relationship  between the extinction coefficient (k) and wave length(λ) of the PS- TiO2 composites

Photon energy(eV)

Figure (4) the relationship between (αhv)1/2(cm-1.eV)1/2  and photon energy of PS- TiO2 composites  for 60 wt..% TiO2

Figure (6) the relationship between (αhv)1/3(cm-1.eV)1/3                     and photon energy of of PS- TiO2 composites  for 20 wt.% TiO2               .

Figure (7) the relationship between (αhv)1/3(cm-1.eV)1/3      and photon energy of of PS-TiO2 composites  for 60wt..% TiO2

(αhv)1/3(cm-1.eV)1/3

wavelength (nm)

Figure(1): Optical Absorbance for PS composite with          various TiO2 concentration.

Photon energy(eV)

Figure (2) the relationship between (αhv)1/2(cm-1.eV)1/2  and photon energy of pure polymer (PS).

K

Photon energy(eV)

(αhv)1/2(cm-1.eV)1/2

(cm)-1α

Photon energy(eV)

Figure (1)  the relationship  between the absorption coefficient and photon energy of the PS- TiO2 composites

(αhv)1/2(cm-1.eV)1/2