Electronic structure of aluminum arsenide nanocrystals

Using Ab initio large unit cell method

Hamad R. Jappor

College of Education, University of Babylon.

Zeyad Adnan Saleh

College of Science, Al-Mustansiriya University.

Mudar A. Abdulsattar

Ministry of Science and Technology.

Abstract

The ab initio restricted Hartree-Fock method is used to simulate the electronic structure of aluminum arsenide nanocrystals consists of (216-738 atoms) with sizes ranging up to about 2.5 nm in diameter. The calculations are divided into two parts, surface and core. The oxygenated (001)-(1×1) facet that expands with larger sizes of nanocrystals is investigated to determine the rule of the surface in nanocrystals electronic structure. Results show that lattice constant and ionicity of the core part are decreasing by increasing the size of nanocrystals. The smallest investigated nanocrystal is 1.83% larger in lattice constant and 13.5% larger in ionicity than the converged value of largest investigated nanocrystal. Increasing nanocrystals size also resulted in an increase of core cohesive energy (absolute value), increase of core energy gap, and increase of the core valence bandwidth. The surface states are found mostly non-degenerated because of the effect of surface discontinuity and oxygen atoms. The method shows fluctuations in the converged energy gap, valence bandwidth and cohesive energy of core part of nanocrystals duo to shape variation. The present work suggests the addition of ionicity and lattice constant to the quantities that are affected by quantum conﬁnement phenomenon. The method of the present model has threefold results; it can be used to approach the electronic structure of crystals bulk, surface, and nanocrystals.

الخلاصة

استعملت طريقة المبادئ الأساسية المحددة لهارتري- فوك لمحاكاة التركيب الإلكتروني لبلورة فوسفيد الألمنيوم النانوية مكون ما بين 216 و 738 ذرة  بقطر يصل إلى nm2.5. قسمت الحسابات إلى جزئيين هما السطح والقلب. وقد درس الوجه المؤكسد (001)-(1x1 ) والذي يتوسع بزيادة حجم البلورة النانوية لتحديد دور السطح في التركيب الإلكتروني للبلورات النانوية. أظهرت النتائج ان ثابت الشبيكة والأيونية للقلب تتناقص بزيادة حجم البلورات النانوية. ان ثابت الشبيكة للبلورة النانوية الأصغر قيد الدراسة اكبر بمقدار 1.83% والتأينية اكبر بمقدار 13.5% من قيمهما في البلورة النانوية الأكبر. بينت النتائج أيضا ان زيادة حجم البلورة النانوية في القلب يؤدي إلى زيادة طاقة الترابط ( القيمة المطلقة)، زيادة فجوة الطاقة، و زيادة عرض حزمة التكافؤ. ولقد بينت النتائج أن حالات السطح تكون قليلة التحلل قياسا بالقلب بسبب عدم استمرارية السطح ووجود ذرات الأوكسجين.

أظهرت الطريقة تقلبات في تقارب فجوة الطاقة وعرض حزمة التكافؤ وطاقة الترابط للقلب، نتيجة لتغيرات شكل البلورة. العمل الحالي يقترح إضافة الأيونية وثابت الشبيكة للكميات التي تتأثر بظاهرة الحصر (التقييد) الكمي. ان طريقة النموذج الحالي لها ثلاث استعمالات ؛ فهي يمكن ان تستعمل للحصول على التركيب الإلكتروني للمادة الصلبة و للسطح و للبلورات النانوية.

1   Introduction

Aluminum arsenide (AlAs) is one of the most important electronic and optoelectronic materials because of its frequent incorporation into GaAs-based heterostructures [Vurgaftman et al., 2001; Adachi, 1994]. AlAs is a wide-gap semiconductor with a band structure and crystallize in the zinc blende. Measurements have revealed a camel’s back structure near X. The  two semiconductors AlAs  and AlP  form  a  continuous  series  of  alloys  denoted  by AlAs1-xPx,  where  x  is  the  mole  fraction  of  AlAs  in  the alloy [Badi et al., 1994], AlAs/AlP superlattices are attractive due to their potential applications in optoelectronic devices because they are expected to become direct band gap materials [Ohnuma and Nagano, 2000].

AlAs is a subject of extensive theoretical studies ranging from the semiempirical to the first principles methods [Mujica et al., 2003], within the density functional theory framework using both pseudopotential [Mujica et al., 1999], and all-electron approaches. For the bulk properties of AlAs, theoretical calculations based on, the Hartree-Fock [Froyen and Cohen, 1983], and potential model [Jivani et al., 2005] have obtained a very good description of its structural and electronic properties. Recently, Annane et al. [Annane et al., 2010] investigated the structural and electronic properties of AlAs and AlP compounds using the full potential linearized augmented plane wave plus local orbitals method based on density functional theory.

The present work addresses large NCs that have the size range of 216–738 total atoms. These atoms are divided between core and surface. The present lower limit (of atoms) is chosen since it provides the first occurrence of idle core part [nearly ideal zinc blende (ZB) structure] that is far from surface reconstruction by more than three surface layers.

In the present work, we study the electronic structure and physical properties of AlAs NCs core and surface part with different sizes by using an ab initio restricted Hartree-Fock (RHF) method coupled with large unit cell method (LUC-RHF). LUC method was formulated and used before for several kinds of bulk materials including diamond and ZB structured materials [Abdulsattar and Al-Bayati, 2007; Harker and Larkins, 1979].

2   Computational details

Ab initio self-consistent Hartree-Fock (RHF) is used to obtain AlAs NCs molecular orbitals. Correlation corrections are neglected in the present calculations relying on Koopmans theorem [Hehre et al., 1986]. This theorem states that  comparisons of Hartree-Fock closed-shell results (which is the  case in the present work) with experimental values suggest that in many cases the energetic corrections due to relaxation effects nearly cancel the corrections due to electron correlation. Simple STO-3G basis [Hehre et al., 1969, Collins et al., 1974] is used in the present work to reach higher number of core and surface atoms.

This method uses (k= 0) approximation, where k is the wave vector, that is one point in the wave vector space. The LUC method is one kind of supercell methods with the above k = 0 restriction. In this method, instead of adding more k points, the single central cell is expanded to contain more atoms, which are now called core atoms in the present work. The LUC method was first suggested and applied to covalent semiconductors in the 1970s [Dobrotvorskii and Evarestov, 1974]. The method was found suitable for NCs calculations because the k = 0 approximation retains only one central cluster of atoms surrounded by other atoms to passivate the outer dangling bonds. The method is used to simulate parts of specific symmetry in the NCs in the same way it is used for bulk materials.

We used 3D PBC (Periodic Boundary Condition) method in GUSSIAN 03 code [Gaussian 03, 2003] to calculate ab initio restricted Hartree-Fock electronic structure of AlAs NCs internal core. The 2D PBC calculations are used to simulate oxygenated (001)-(1×1) surface.

In the present work, we divided the work into two parts, core and surface parts which is the traditional method used in microscopic-size solid-state calculations. In LUC core part only the lattice constant is optimized, at the surface part all bond lengths and lattice constant still need to be optimized because of surface reconstruction. The (001) chosen surfaces are terminated by oxygen atoms to passivated dangling bonds. The width of surface part is set to one conventional lattice that is deduced from AlAs surface bonds calculations. The oxygenated (001)-(1×1) AlAs surface in the oxygen double bonding configuration is investigated to obtain the total electronic structure of the AlAs NCs with (001)-(1×1) facets. The oxygenated (001)-(1×1) AlAs surface is chosen since it is one of the least reconstructed surfaces. Unlike the core part, the bond lengths and lattice constant are not unique and a variation of geometrical parameters is needed. Normally surface effects do not penetrate more than four layers (one lattice constant) from the crystal surface [Kittel, 1976]. On the other hand, short-range sp3 bonds do not require more than fourth neighbor’s interaction range to conduct electronic structure calculations successfully using molecular orbital methods. The upper two identical conditions are applied in the present calculations.

Two kinds of core LUCs are investigated, namely cubic and parallelepiped cells. The cubic cells are multiples of ZB structure Bravais unit cells, while the parallelepiped cells are multiples of primitive ZB structure unit cells [Kittel, 1976]. Cubic core cells include 8, 64 atoms. Parallelepiped cells include 16, 54, 128 atoms.

3   Calculations and results

In this section, we present the calculated band structures of aluminum arsenide nanocrystals. Figure (1) shows the total energy for AlAs nanocrystal as a function of lattice constant for 8 core atoms, from which we obtained the equilibrium lattice constant. Figure (2) shows the variation of the lattice constant of AlAs NCs core as a function of number of core atoms. This figure is obtained after minimizing the energy lattice curve of every investigated number of core atoms. From this figure we see that the lattice constant for the core part of the crystal decrease with increasing number of atoms, the lattice constant for AlAs NCs shows decreasing values from 0.555 nm for 8 atoms to 0.545 nm for 64 atoms LUC, then the lattice constant tends to be constant for LUC of atoms number greater than 64. The converged lattice length for a high number of core atoms (0.545nm) is found to be close to the lattice constant values of 0.562 nm for bulk [Zhu and Louie, 1991].

Figure (1): Total energy of 8 AlAs core atoms as a function of lattice constant.

Figure (2). Energetically optimized AlAs core lattice constant as a function of the number of atoms in the core.

The bulk modulus has been calculated from Cohen’s theory [Kaxiras, 2003]:

where NC is the coordination number (= 4),  is s a dimensionless number which describes the ionicity: (= 0, 1 and 2 for IV, III-V and II-V groups respectively) [Zheng et al., 1999],  is the first-neighbor distance in Å, i.e., the interatomic distance, for the ZB structure we have [Adachi, 2009]:

Bulk modulus of AlAs nanocrystal as a function of number of atoms in the core is shown in Figure (3). This Figure shows that the bulk modulus increases with the number of atoms in the core. This relation can be simply attributed to the fact that the lattice constant for the core part of the crystal decrease with increasing number of atoms, the latter equation means that the decrease in lattice constant entails a decrease in interatomic distance (d) which leads to increasing in the bulk modulus according to equation (1).

We note that the bulk modulus for AlAs nanocrystal of 81.39GPa is in a good agreement with the experimental value of 82 GPa [Hellwege and Madelung, 1982] of the bulk taking into consideration that Hartree-Fock theory always overestimates bulk modules values [Abdulsattar and Al-Bayati, 2007].

Figure (3): Bulk modulus as a function of the number of core atoms for AlAs NCs.

AlAs has an indirect minimum gap with the CBM at X point of the Brillouin zone. Figure (4) shows the energy gap of the core part of the investigated nanocrystals against the number of core atoms. In nanostructures, normally, the dimensions are commensurate with the de Broglie wavelength of the charge carriers; so that quantum confinement effects become important and the properties of the semiconductors are significantly modified. Due to the quantum confinement effect, the energy band gap of nanocrystals decreases with increasing the size of the quantum structure [Bruno et al., 2005].The increase of the energy gap in the first part of the considered range is not a violation of the quantum confinement theory since the energy gap is controlled by the surface part gap [Aysa et al., 2011], which is much smaller gap than the core part as we seen shortly. All energies converge quickly for the nanocrystals with more than 64 core atoms with a very wide energy gap variation range approximately (4.50 - 5.33)eV; this convergence is associated with fluctuations depending on the geometry of the nanocrystal core. Figure (4) shows that the size of the cell has no pronounced effect on the electronic structure of the core of nanocrystals in the large number of atoms, whereas the effect of size is more pronounced in the case of small LUC size (8, 16, and 54 atoms) this is also found in [Chelikowsky, and Saad, 2004]. The energy gap is higher than the experimentally reported energy gap (2.25 eV) for bulk AlAs [Vurgaftman et al., 2001] but within the trends of nanocrystals blue shift [Shimazaki and Asai, 2010; Nama et al.,, 2010]. At the SCF level, Koopmans’ theorem holds, and the task of determining the band energies and energy gap can be reduced to ﬁnding the one-electron energies of the respective Bloch states. It is well known that SCF (HF) calculations tend to overestimate the energy gap, giving too low an energy for the top of the upper valence band and too high an energy of the conduction band bottom. The reason for this is that HF theory optimizes a wavefunction. So, to determine the same property using a wavefunction, we need to know the correct quantum mechanical operator. HF orbitals, experience varying potentials, and, in particular, HF virtual orbitals experience the potential that would be felt by an extra electron being added to the molecule. As a result, HF virtual orbitals tend to be too high in energy and anomalously diﬀuse. This fact is especially important for crystalline solids and explains why HF band gaps are overestimated compared to those in experiment and other ab initio methods .This convergence is associated with fluctuations depending on the geometry of the nanocrystal core.

Figure (4): Energy gap of the core part of AlAs nanocrystals as a function of the number of core atoms.

The present cohesive energy (Figure (5)) of 8 atom large unit cell of AlAs NCs (15.057eV) is approximately 99.15% larger than the experimental value (7.56 eV) reported by Harrison[Harrison, 1989] and 88.21% larger than the experimental value (8eV) Paulus for bulk [Paulus, 1996].

These values of cohesive energy belong not to the nanocrystals as a whole but to the core only since the surface consists of two kinds of atoms and when the researcher add the surface effect we expect that the cohesive energy will be reduced to the experimental value and this is not done in the present work since it takes very long time and a lot of memory out of the disk space.

In present work, we calculated valence bandwidth which is the difference between the highest occupied molecular orbital (HOMO) and lowest unoccupied molecular orbital (LUMO). The valence bandwidth as a function of number of atoms for AlAs nanocrystal core part is shown in Figure (6). One can see from the figure that this band generally increases with increasing number of atoms and become nearly stable at the 64 core atoms.

At the HF level, Koopmans’ theorem suggests that the energy of the HOMO is a good approximation to the negative experimental ionization potential. Similarly, it suggests that the electron affinity for an Ne-electron system is equal to the negative of the LUMO energy [Sque et al., 2006], assuming that the orbitals do not relax. Figure (7) shows the variation of HOMO and LUMO as the core of nanocrystals grows up in size and changes its shape. This curve fluctuates strongly because of the change in size and shape that produces different surfaces with different properties. Not all quantities have definite convergence behaviour similar to the upper investigated quantities.

Figure (5): Cohesive energy of the core part of AlAs NCS as a function of the number of core atoms.

Figure (6): Valence bandwidth of the core part of AlAs nanocrystals as a function of core atoms.

HOMO and LUMO energy levels plotted in Figure (7) show fluctuating behaviour that continues indefinitely. As nanocrystals grow up in size they develop different shapes and surfaces. Each of the developed surfaces has different properties such as the upper mentioned ionization potential and affinity or HOMO and LUMO energy levels. Therefore, these fluctuations start at the nano-scale, continue to the micro, and bulk scale. A similar behaviour is observed for SiGe nanocrystals [Abduljalil et al., 2011].

Figure (7): HOMO and LUMO energies that correspond to different core sizes of AlAs nanocrystals.

The ionicity charge is calculated as a function of number of atoms using Gaussian program as shown in Figure (8), which is shows that the ionicity charge decrease with increasing number of atoms for core part; smaller nanocrystals are more ionic than larger ones ionicity nearly converges after 64 core atoms to nearly 0.39. This behaviour is encountered not only for the ionicity but also for the energy gap and lattice constant. However, the ionic charge of aluminum atoms equal ionic charge of arsenide atoms and the net charge equals to zero.

Figure (8): Ionicity of the core part of AlAs nanocrystals as a function of the number of core atoms.

Figure (9): Degeneracy of states of 8 atoms core part of AlAs nanocrystal as a function of energy levels.

The degeneracy of energy level states for AlAs nanocrystal as a function of levels energy for the lowest energy lattice constant is calculated for core and surface parts. Figure (9) shows the degeneracy of states for 8 atoms of core part. Due to high symmetry, the number of degenerate states is high in the core part. The highest number of degenerate states in the valence band is between 6 for the 8 atom core. A similar behaviour is observed for diamond nanocrystals ab initio large unit cell calculations [Abdulsattar, 2011].

To investigate nanocrystals surface electronic structure, it is natural to assume that larger nanocrystals to have larger surfaces. Two oxygenated oxygen terminated (001)-(1×1) AlAs surface stoichiometry slabs are investigated, namely, Al8O4As8, and Al32O16As32 with two surface areas of a2, and 4a2 respectively where (a) is the lattice constant.

The average lattice constants of the two investigated stoichiometries are less than the corresponding core parts, but they follow the same decreasing order. The oxygenated (001)-(1×1) surface slab calculations of the nanocrystal converge to approximately the same lattice constant value of the core (0.57 nm). This good matching between surface and core lattice constants shows that good adhesion is expected between the two parts.

The energy gap of (001)-(1×1) oxidized surface show much smaller gap than that of the core part. Oxidised surface gap of AlAs calculated using slab geometry of the stoichiometry Al8O4As8 is 0.113 eV. This value is very near to the oxidised germanium surface gap 0.19 eV calculated using the same geometry [Aysa et al., 2011]. The same surface for silicon has 1.4 eV [Nama et al., 2010]. From these values we can conclude that the oxidised AlAs surface part of nanocrystals is the governor of the energy gap value and that the variation of the core part gap in Figure (4) does not alter ﬁnal gap value. Figures (10) represent the degeneracy of states for oxygenated (001)-(1×1) surface part of Al8O4As8 stoichiometry slab nanocrystal surface. This surface has lower number of degenerate states compared with core part of Figure (9). This low degeneracy is due to broken symmetry at the surface discontinuity. The existence of oxygen atoms leads to varying the bond lengths and lattice constant.

Figure (10): Degeneracy of states of surface part of Al8O4As8 stoichiometry slab as a function of energy levels.

In the surface part, discontinuity of surface imposes level splitting on the degenerate energy levels. The splitting of energy levels dose not only affects the number of degenerate states, but also the valence bandwidths which is wider in surface part. On the other hand, the splitting of states and additional oxygen surface states strongly affect the energy gap and considerably reduce its value.

4   Conclusions

In this paper, we studied some properties of AlAs nanocrystals. The total energy, lattice constant, bulk modulus, cohesive energy, energy gap, valence bandwidth, ionicity, and degeneracy of energy levels have been calculated by the self-consistent restricted Hartree–Fock method coupled with the large unit cell method (RHF-LUC). From the results as discussed the following points were concluded:

- The present results reveal that the electronic properties converge to some limit as the size of the LUC increases.

- The total energy (absolute value) of nanocrystal increases with the increase of number of LUC for core and surface part.

- The lattice constant decreases with increasing the number of atoms in the LUC until we reached 64 atoms, beyond this point any increase in the number of atoms does not affect the lattice constant. The lattice constant of core part is larger than the lattice constant of the surface part that induces stresses on both core and surface.

- Surface and core parts have approximately the same lattice constant that reflects the good adherence of oxide layer at the surface. The equilibrium lattice constant in reasonable agreement with the experimental data.

- The bulk modulus increases with increasing the number of atoms in the LUC until we reached 64 atoms, beyond this point any increase in the number of atoms does not affect the bulk modulus. The calculated bulk modulus in good agreement with the experimental results of bulk.

- The cohesive energy (absolute value)  increases as the number of atoms in the LUC increases until we reached 64 atoms, beyond this point any increase in the number of atoms does not affect the cohesive energy (cohesive energy become constant).

- The energy gap is controlled by the surface part of the nanocrystal. Energy gap increases with increasing size of LUC for core and surface part and the values of energy gap for surface part are less than comparable values of energy gap for core part.

- Valence bandwidth increases with increasing size of LUC for core and surface part, valence bandwidth in surface part is larger than for core part caused by the existence of oxygen atoms.

- The degeneracy of states of core part for all sizes of LUC is larger than the degeneracy of surface part.

- The present work suggests the inclusion of lattice constant, ionicity and other properties to the quantum conﬁnement affected properties that already include energy gap of nanocrystals.

5   References

Abduljalil, H.M., Abdulsattar, M.A., and Al-Mansoury, S.R., 2011 "SiGe nanocrystals core and surface electronic structure from Ab initio large unit cell calculations", Micro&Nano Lett. Vol.6, p.386.

Abdulsattar, A., and Al-Bayati, K., 2007,"Corrections and parameterization of semiempirical large unit cell method for covalent semiconductors", Phys. Rev. B Vol. 75, p 245201-1.

Abdulsattar, M. A., 2011, "Ab initio large unit cell calculations of the electronic structure of diamond nanocrystals", Solid State Sciences Vol.13, p.843.

Adachi, S., 1994,"GaAs and Related Materials: Bulk Semiconducting and Superlattice Properties", World Scientiﬁc, Singapore.

Adachi, S., 2009, "Properties of semiconductor alloys: group-IV, III–V and II–VI semiconductors", John Wiley & Sons Ltd, Chichester.

Annane, F., Meradji, H., Ghemid, S., and Hassan, F. E., 2010, "First principle investigation of AlAs and  AlP compounds and ordered AlAs1-xPx alloys ",Computational Materials Science Vol.50, p.274.

Aysa, N. H., Abdulsattar, M.A., and Abdul-Lettif, A.M., 2011, "Electronic structure of germanium nanocrystals core and (001)-(1×1) oxidised surface", Micro&Nano Lett. Vol. 6, p.137.

Badi,N., Abid, H., Soudini, B., Amrane, N., Driz, M., Khelifa B. and Aourag, H., 1994, "Valence and conduction band-edges-charge densities in Ga1-xAlxP mixed crystals", Materials Chemistry and Physics Vol.38, p.243.

Bruno, M., Palummo, M., Marini, A., Del Sole, R., Olevano V., Kholod, A. N., and Ossicini, S.,2005, "Excitons in Germanium Nanowires: Quantum Confinement, Orientation, and Anisotropy Effects within a First-Principles Approach", Phys. Rev. B Vol. 72, p.153310.

Chelikowsky, J. R., and Saad, Y., 2004, "Electronic Structure of Clusters and Nanocrystals", University of Minnesota.

Collins, J. B., Schleyer, P. V., Binkley, J. S., and Pople, J. A.,1976, "Self consistent molecular orbital methods. XVII. Geometries and binding energies of secondrow molecules. A comparison of three basis sets" J. Chem. Phys. Vol.64, p.5142.

Dobrotvorskii, A.M. and Evarestov, R.A., 1974, " The Quasi-Molecular Large Unit Cell Model in the Theory of Deep Levels in Imperfect Crystals:  Point Defects in Graphitic Boron Nitride" Phy. Sta. Sol. (b) Vol.  66, pp. 83-91.

Gaussian 03, Revision B.01, M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria, M. A. Robb, J. R. Cheeseman, J. A. Montgomery, Jr., T. Vreven, K. N. Kudin, J. C. Burant, J. M. Millam, S. S. Iyengar, J. Tomasi, V. Barone, B. Mennucci, M. Cossi, G. Scalmani, N. Rega, G. A. Petersson, H. Nakatsuji, M. Hada, M. Ehara, K. Toyota, R. Fukuda, J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai, M. Klene, X. Li, J. E. Knox, H. P. Hratchian, J. B. Cross, C. Adamo, J. Jaramillo, R. Gomperts, R. E. Stratmann, O. Yazyev, A. J. Austin, R. Cammi, C. Pomelli, J. W. Ochterski, P. Y. Ayala, K. Morokuma, G. A. Voth, P. Salvador, J. J. Dannenberg, V. G. Zakrzewski, S. Dapprich, A. D. Daniels, M. C. Strain, O. Farkas, D. K. Malick, A. D. Rabuck, K. Raghavachari, J. B. Foresman, J. V. Ortiz, Q. Cui, A. G. Baboul, S. Clifford, J. Cioslowski, B. B. Stefanov, G. Liu, A. Liashenko, P. Piskorz, I. Komaromi, R. L. Martin, D. J. Fox, T. Keith, M. A. Al-Laham, C. Y. Peng, A. Nanayakkara, M. Challacombe, P. M. W. Gill, B. Johnson, W. Chen, M. W. Wong, C. Gonzalez, and J. A. Pople, Gaussian, Inc., Pittsburgh PA, (2003).

Froyen, S., Cohen, M., 1983,"Structural properties of III-V zinc-blende semiconductors under temperature", Phys. Rev. B Vol. 28, p. 3258.

Harker, A. H., and Larkins, F. P., 1979,"A large unit cell semiempirical molecular orbital approach to the properties of solids. II. Covalent materials: diamond and silicon" J. Phy. C : Solid State Phys. Vol. 12, p.2497.

Harrison, W.A., 1989,"Electronic Structure and the Properties of Solids: The Physics of the Chemical Bond", Dover Publications, Inc., New York.

Hehre, W., Radom, L., Schleyer, P., and Pople, J., 1986,"Ab Initio Molecular Orbital Theory", John Wiley & Sons, New York.

Hehre, W., Stewart, R. F. and Pople, J. A., 1969, "Self Consistent Molecular Orbital Methods. I. Use of Gaussian Expansions of Slater Type Atomic Orbitals", J. Chem. Phys. Vol.51, p.2657.

Hellwege,K.-H., and Madelung, O., (Eds.), 1982, "Semiconductor, Intrinsic Properties of Group IV Elements and III-V, II-VI and I-VII Compounds", Landolt-Bornstein New Series, Group III, Vol. 22, Pt Springer, Berlin.

Jivani, A., Trivedi, H., Gajjar, P. N.,and Jani, A., 2005 "Total energy, equation of state and bulk modulus of AlP, AlAs and AlSb semiconductors", Pramana-J. Phys. Vol. 64, p.153.

Kaxiras, E., 2003,"Atomic and Electronic Structure of Solids", Cambridge University Press, New York.

Kittel, C., 1976, "Introduction to Solid State Physics", John Wiley & Sons, New York, USA, 5th edn.

Mujica, A., Rodríguez-Hernández, P., Radescu, S., Needs, R. J., and Muñoz, A., 1999, "AlX (X = As, P, Sb) Compounds under Pressure", phys stat sol. (b) Vol.211, p.39.

Mujica, A., Rubio, A., Muńoz, A., and Needs, R. J., 2003,"High – pressure phases of group–IV, III-V, and II-VI compounds", Rev. Mod. Phys. Vol. 75, p. 863.

Nama, N.A., Abdulsattar, M.A., and Abdul-Lettif, A.M., 2010,"Surface and core electronic structure of oxidized silicon nanocrystals", J. Nanomater., 2010, article ID. 952172, 6 pages.

Ohnuma, T., and Nagano, M., 2000, Jpn. J. Appl. Phys. Vol.39, p.L972.

Paulus, B. Fulde P., and Stoll, H., 1996,"Cohesive energies of cubic III-V semiconductors", Phys. Rev. B Vol.54, p.2556.

Shimazaki, T., and Asai, Y., 2010 "Energy band structure calculations based on screened Hartree–Fock exchange method: Si, AlP, AlAs, GaP, and GaAs", J. Chem. Phys. Vol. 132, p. 224105.

Sque, S.J. Jones, R., and Briddon, P.R., 2006, "Structure, electronics, and interaction of hydrogen and oxygen on diamond surfaces", Phys. Rev. B Vol.73, p.085313.

Vurgaftman, I., Meyer, J. R., and Ram-Mohan, L. R., 2001,"Band parameters for III–V compound semiconductors and their alloys", J. Appl. Phys. Vol.89, p. 5815.

Zheng,J. C., Huan, C.H., Wee, A. T ., Wang, R.Z., and Zheng, Y.M.,1999, J Phys: Condens Matter Vol. 11, p.927.

Zhu,  X. and Louie, S. G.,1991, Phys. Rev. B Vol. 43, p.14142.