Study on the Stop Crack growth for shaft by using Drilling Hole

Ouday kudom  Mohammad

Abstract

The aim of this search is study the effect of the hole for control on crack growth for the rotation shaft ,provide rotating shaft in which test work is applied , provide the electrical drill for drilling , the shaft at crack tip .the test of rotating solid   shaft for five months , whine the measure  the length and depth hole thickness of the crake within time ,The purport of the hole in the crack tip is distribution the in eternal  stresses constrictions for decrease ,The applied force on the crack The applied force(F) at the crack tip is convert into two components angel( 45) normal and tangential force (F1&F2),The normal force is less than ,the applied force ,in this case prevent the shaft form failure by using the suitable  diameter and depth of the hole for stop of crack growth and kept the continues work

الخلاصة

الهدف من هذا البحث هو دراسة تأثير الثقب للسيطرة على نمو الشق لعمود دوران حيث تم تهيئة عمود دوران ,تتم علية أجراء الاختبارات ومثقب كهربائي  لأجراء ثقب العمود عند نهاية الشق .تم الاختبار على عمود دوران حديد و لمدة خمسة اشهر . حيث وجد ازدياد عمق وسمك وطول الشق بمرور الزمن , ان فائدة الثقب في نهاية الشق هو توزيع الأجهادات المتمركزة الداخلية مما يؤدي إلى تقليل القوة المسلطة على الشق(  ) حيت تم في هذة الحالة تحليل المركبة العمودية  إلى مركبتين وبزاوية 45درجة نظريا(  &   )القوة العمودية هي اكبر من القوة الجانبية التي تم تحليلها وهذا ماثبت خلال الجانب العملي بمرور الزمن لحالة تم الحفاظ على العمود من الفشل من خلال التوصل إلى قطر وعمق ثقب مناسب لغرض إيقاف الشق للحفاظ على استمرار العمل

Introduction

Stress Concentration

When an axial load is applied to a piece of material with a uniform cross-section, the normal stress will be uniformly distributed over the cross-section. However, if a hole is drilled in the material, the stress distribution will no longer be uniform ( kormay & Disnig, 1991; Ack, et  at ; 1988).Since the material that has been removed from the hole is no longer available to carry any load, the load must be redistributed over the remaining material.  It is not redistributed evenly over the entire remaining cross-sectional area but instead will be redistributed in an uneven pattern that is highest at the edges of the hole as shown  Fig.1. This phenomenon is known as stress concentration

| . Drill hull Fig (1) stress concentration due to a hole ( kormay & Disnig, 1991 ). |  |
| --- | --- |

concept has been successfully used with stress-intensity factors to predict the growth of cracks under a wide variety of load histories and in complex crack configurations. Both test and crack-closure analyses have shown that the stress-intensity-factor-range-against-rate curves are affected by the stress ratio ®, the applied stress or load level (Smax or Pmax), and the crack-front constraint (plane-stress or plane-strain behavior). However, most life-prediction codes use only linear-elastic fracture mechanics (LEFM) concepts, which neglect stress-level effects,. Thus, under some loading conditions, such as negative R ratios or high-applied stress levels, non-conservative life predictions are made using only  (Savarge , 2007)procedures. Fatigue-crack-growth tests have been conducted on middle-crack tension M(T) specimens made of thin-sheet (B = 2.3 mm) aluminum alloy over a wide range in applied stress levels (0.1–0.5 times the flow stress of the material) and for two stress ratios (R = 0.05 and ?1). The FASTRAN life-prediction code, using either the crack-closure model or LEFM procedures, and the AFGROW code, which uses only LEFM procedures, were used to make crack-growth predictions from an initial crack size to failure in the M(T) specimens. The results from AFGROW and FASTRAN, using LEFM procedures, agreed very well with each other. The crack-closure model predicted all results with ±20%, whereas, the codes using  (Ehrabian & Sci 1999; Joly and Mehrabian,2003) procedures (neglecting stress-level effects) resulted in non-conservative life predictions as large as a factor-of-3 from the test results For some components the crack propagation life is neglected in design because stress levels are high, and/or the critical flaw size small. For other components the crack growth life might be a substantial portion of the total life of the assembly. Moreover, preexisting flaws or sharp design features may significantly reduce or nearly eliminate the crack initiation portion of the fatigue life of a component. The useful life of these components may be governed by the rate of sub critical crack propagation,Aircraft fuselage structure is a good example of structure that is based largely on a slow crack growth rate design. Many years ago,   (G.M Savaged , 2007) reviewed a great number of malfunction reports from a variety of aircraft. The reports showed that the preponderance of structural failures occurred from 1) built-in preload stresses, 2) material flaws and 3) flaw caused by in-service usage(.J.oly; P2006). These facts led to a design approach that required the damage tolerance analysis to assume a material flaw exists in the worst orientation and at the most undesirable location. The analysis helps to ensure that structures are designed that will support slow stable crack growth until the crack reaches a length where it can reliable be detected using NDT methods. The rate of fatigue crack propagation is determined by subjecting fatigue-cracked specimens, like the compact specimen used in fracture toughness testing, to constant-amplitude cyclic loading. The incremental increase in crack length is recorded along with the corresponding number of elapsed load cycles acquire stress intensity (K), crack length

Q max = Kt * Q nom

The first mathematical treatments of stress concentrations were published in 2000. Closed form solutions are available for the very simple geometries. However, for more complex cases, experimental methods for measuring highly localized stresses (photo elastic tests, precision strain gage tests, membrane analogy for torsion, etc.) and computerized finite element solutions have been used. The results of the studies are available in the form of published graphs. This module uses polynomial and power regression curve fitting to approximate close form solutions of the graphs. These approximations are within 1% of the Kt value read directly from the graphs in the references. Note that the stress concentration graphs are theoretical factors based on a theoretical homogenous, isotropic, and elastic material. Real materials have microscopic irregularities causing a certain no uniformity of microscopic stress distribution, even in notch-free parts. Thus, the addition of a stress raiser (notch, hole, etc.) may not cause as much additional damage as indicated by the theoretical factor. The ductility or brittleness of the material has a pronounced effect on its response to stress concentrations under static loads. Stress concentration will cause failure of brittle materials if the concentrated stress is larger than the ultimate strength of the material. In ductile materials, concentrated stresses larger than the yield strength will generally cause local plastic deformation and redistribution of stresses (renderingthem more uniform). Thus, it is common to ignore the effects of geometric stress concentration in ductile materials under static loading. The stress for the net cross section is calculated as if the stress concentration were not there (the stresses are larger than for an unnoticed part of the same overall dimensions because the smaller net cross-sectional area is used). Areas of stress concentration are possible sites for fatigue if the component is cyclically loaded (even for ductile materials). the image. Region I is the fatigue threshold region where the Dk is too low to propagate a crack. Region II encompasses data where the rate of crack growth changes roughly linearly with a change in stress intensity fluctuation. In region III, small increases in the stress intensity amplitude, produce

Fig (2) number of cycles (G.M Savage , 2007)

Drilling  hole	crack

Fig (3) Drilling  hole

z=ll / 32 ×d

A   B      C         D	E

D

Fig (4) Drilling  hole stap by

Kt= Q max/ Qnom

Table (1)   of  node the crack for length

Equations

Variables:

Kt = Theoretical Stress Concentration Factor

Q max= Stress Concentration at design ,max Stress

Q nom= Stress Concentration at ,p/A , for A=11/ 4 (d)

S1 = Biaxial Stress Normal to the Major Axis

S2 = Biaxial Stress Parallel to the Major Axis

r = Fillet or Notch Radius

D = Large Dimension

| No.1 month | 0,5 | A |
| --- | --- | --- |
| No.2 month | 0,8 | B |
| No.3 month | 1 | C |
| No.4 month | 1,5 | E |
| No.5 month | 2 | F |
| month | Crack length( mm) | No. |

practical side

The work test include the rotating shaft with uniform rotating speed is simply supported on the ball bearing containing circum France crack due to the shear stress result from rotating .The electrical drill with variable diameter of drills shown in table (2) the hole of shaft is done at crack tip and measure the diameter and depth the hole .The hole diameter is increase at the beginning energy month  for five months to get the the suitable hole diameter the crake growth stopped on it

Table (2): practical side drilling ,crack

| Drill depth | Diameter crack | depth crack | crack thickness |
| --- | --- | --- | --- |
| 2,5mm | 3mm | 0,5mm | 0,01mm |
| 3,4mm | 4mm | 0,8mm | 0,02mm |
| 3,6mm | 5mm | 1mm | 0,03mm |
| 4mm | 6mm | 1,2mm | 0,04mm |
| 4,5mm | 7mm | 1,5mm | 0,05mm |
| 6,8mm | 8mm | 1,9mm | 0,06mm |
| 8,7mm | 9mm | 2mm | 0,07mm |
| 10,5mm | 10mm | 2,4mm | 0,08mm |
| 12,5mm | 12mm | 2,5mm | 0,09mm |
| 15,25mm | 14mm | 3mm | 0,1mm |
| 17mm | 16mm | 3,5mm | 0,19mm |
| 18mm | 18mm | 4mm | 0,2mm |

Force of crake equation assume O=45

F1 =Fn cosO

F2=Ft sinO

F > Fn cosO

F> Ft sinO

f 1	f2

Drilling  hole

F	F

f 1	f2	f2	f 1

Fig (4) Drilling  hole Stress Concentration

| d /D | 0.02 | 0.04 | 0.08 | 0.10 | 0.16 |
| --- | --- | --- | --- | --- | --- |
| kt | 2.70 | 2.56 | 2,33 | 2.26 | 2,11 |

Table (3) :Theoretical stress concentration factor( kt) for a plate with hole of diameter d in bending( kormay & Disnig, 1991; Ack, et  at ; 1988).

Discussion & Results

1-The applied force(F) at the crack tip is convert into two components normal and tangential force ,The normal force is less than ,the applied force as shown in the fig.(4)

2-the length ,depth of the crake will increase for the severe month at Uniform rotating speed .

3-The crack growth decrease with increase diameter hole .

4-The crack growth before drilling is proposition with time.

5-un uniform of the increase of crack depth is corresponding.

References

Ack , J. E-snell , 1988Towards Vol.4 No 7   pp,48 – 50

G.M Savarge , 2007 metals and materials Vol.2 No4 pp77-84

Joly; P2006.A and R hguytring  mat sci Eng 55  pp 64-66

Kormay k.  1991w,disnig  pp.66-69

P.A.Joly and R mehrabian  mat sci Eng 55 2003 pp34-56

R .M ehrabian 1999,T.U ,Sci   pp,45-565-5

Savarge; 2007G, metals and materials Vol.2 No4  pp77-84

T.O fhjh h.OP 1998Vol 2 No  4  pp,36-45

W.M favgnming , 2004 metals and drilling Vol.2 No1 pp17-18

Journal of Babylon University/ Engineering Sciences / No.(1)/ Vol.(21): 2013

280

279